Data/hora: 26/04/2024 16:02:27

Biblioteca(s): 	Embrapa Caprinos e Ovinos.	
Data corrente: 	05/10/2005	
Data da última atualização: 	01/07/2016	
Autoria: 	DAL MOTE, M. A. de B. L.; COSTA, R. R. G.; JACINTO, M. A. C.; MEDEIROS, A. N. de; FIGUEIREDO, F. das C.	
Título: 	Características físico-mecânicas e químicas do couro de caprinos abatidos em idades diferenciadas.	
Ano de publicação: 	2004	
Fonte/Imprenta: 	Revista Brasileira de Zootecnia, Viçosa, MG, v. 33, n. 5, p. 1285-1291, set./out. 2004.	
Idioma: 	Português	
Conteúdo: 	Objetivando-se analisar as características físico-mecânicas do couro de caprinos, após o curtimento, utilizaram-se 16 animais machos mestiços Alpinos, com idades a partir dos 180 dias de vida, abatidos em intervalos de 45 dias (quatro animais por abate). As peles foram curtidas e recurtidas e dos couros retiraram-se três corpos-de-prova das regiões dorsal, paleta, ventral, anca e lateral,  nas direções paralelas e perpendicular ao eixo crânio-caudal, para realização dos ensaios físico-mecânicos: distensão da "flor" no lastrômetro, rasgamento progressivo, resistência à tração, análises químicas de extração de lipídios, óxido de cromo, pH e cifra diferencial. A idade do animal exerceu efeito positivo no ensaio de resistência à tração, com superioridade para os caprinos de 315 dias de vida. A região e a posição em todos animais estudados apresentaram efeito significativo no ensaio de resistência ao rasgamento progressivo, nas quatro idades, atingindo o valor de referência mínima de 80 kgf/cm. A resistência do couro à distensão da "flor" dos caprinos estudados foi superior ao mínimo de 7 mm, demonstrando grande elasticidade dos couros, sem influência de idade ou região. 

[Physical and Mechanical Characteristics Quality of Goats Leather at Different Ages].
Abstract: This paper focuses on the analysis of goats leather to identify the physical and mechanical characteristics after toning. Sixteen male crossbred Alpine goats, with four animals from 180 days old by slaughter, were used. Slaughter intervals of 45 days were used. The skins were tanned and re-tanned, and from the breather the proofs from the dorsal, palette, ventral, hind and lateral regions, were taken, in the following directions: parallel and perpendicular to the tail-skull axis, so that the physic-mechanic studies could be performed: distention of the "flower" in the lastometer, progressive tearing; resistance to traction and chemical analyses of fat, chrome, pH and differential code. Animal age showed positive effect on traction resistance, with high values to goats at 315 days old. The region and position of all animals studied shower significant effect on the four reach ages, reaching the minimum reference value of 80 kgf/cm. Bather resistance to distention of the "flower" from the goats were superior to the minimum of 7 mm, showing the great elasticity of the bather, with no effect of age or region.	
Thesagro: 	Caprino; Couro; Pele; Qualidade; Resistência.	
Categoria do assunto: 	--	
Registro original: 	Embrapa Caprinos e Ovinos (CNPC)	
Exemplares: 	CNPC - (17996-1) - ADD - AP - -- -  -  - v33,p.1285 - DIS