Data/hora: 25/04/2024 12:37:33

Biblioteca(s): 	Embrapa Agrossilvipastoril; Embrapa Roraima.	
Data corrente: 	01/06/2022	
Data da última atualização: 	11/05/2023	
Autoria: 	PECEGUEIRO, M. de S.; HOOGERHEIDE, E. S. S.; BENDAHAN, A. B.; EVANGELISTA, W. V.; BEHLING, M.	
Afiliação: 	MAICON DE SOUZA PECEGUEIRO, UNEMAT, Alta Floresta-MT; EULALIA SOLER SOBREIRA HOOGERHEIDE, CPAMT; AMAURY BURLAMAQUI BENDAHAN, CPAF-RR; WESCLEY VIANA EVANGELISTA, UNEMAT, Alta Floresta-MT; MAUREL BEHLING, CPAMT.	
Título: 	Calibration of the Pilodyn instrument for the indirect in situ determination of the basic wood density of balsa	
Ano de publicação: 	2022	
Fonte/Imprenta: 	Ciência Rural, v. 52, n. 12, e20210337, 2022.	
ISSN: 	1678-4596	
DOI: 	https://doi.org/10.1590/0103-8478cr20210337	
Idioma: 	Inglês	
Conteúdo: 	Abstract: Balsa wood is used widely in the nautical, aeronautical and wind-energy industries because of its low-density and high-resistance. In the Brazilian state of Mato Grosso, speculative producers with little knowledge of the culture have established balsa plantations using non-standardized and non-selected seedlings. In this sense, research is needed to improve balsa cultivation under Brazilian conditions to better explore the resource. The present study evaluated the efficiency of the Pilodyn instrument for the indirect determination of the basic wood density (BWD) of balsa. Twenty 12-year old balsa trees cultivated in Alta Floresta, Mato Grosso, were probed with the Pilodyn instrument on both north and south faces of the trunk at the base and at 1.30 and 3.10 m from the ground. Wood discs were subsequently collected from the probed sites and BWD determined according to the water-immersion method. Data were submitted to the Shapiro-Wilk normality test followed by analysis of variance and Pearson?s correlation analysis with &#945;=0.05. The BWD of balsa decreased in the direction from the base to the top of the tree. The penetration depth of the Pilodyn probe was inversely proportional to BWD with a correlation that was strong (R2=0.72) at heights of 1.30 and 3.10 m but considered weak (R2=0.46) at the base of the trunk. The reliability of the Pilodyn method was sufficient to allow the development of a linear equation that could be applied for the indirect determination of the BWD of balsa based on the penetration depth of the Pilodyn probe assessed at 1.30 m from the ground. | Resumo: O pau-de-balsa é amplamente utilizado nas indústrias náutica, aeronáutica e de energia eólica devido à sua baixa densidade. No estado de Mato Grosso, produtores especulativos de balsa têm estabelecido plantios sem conhecimento sólido da cultura usando mudas não padronizadas e não selecionadas. Pesquisas são necessárias para melhorar o cultivo de balsa sob condições brasileiras para melhor explorar este recurso. O presente estudo teve como objetivo avaliar a eficiência do instrumento Pilodyn para a determinação indireta da densidade básica da madeira (DBM) de balsa. Vinte árvores de 12 anos de idade cultivadas em Alta Floresta, Mato Grosso, foram avaliadas com o instrumento Pilodyn nas faces norte e sul do tronco, na base e a 1,30 e 3,10 m do solo. Discos de madeira foram posteriormente coletados dos locais sondados e o DBM determinado de acordo com o método de imersão em água. Os dados foram submetidos ao teste de normalidade Shapiro-Wilk seguido de análise de variância e análise de correlação de Pearson com &#945;=0,05. Os valores de DBM da balsa diminuiu da base em direção ao topo da árvore, enquanto a profundidade de penetração do Pilodyn foi inversamente proporcional. A correlação entre a profundidade de penetração do Pilodyn e o DBM foi fraca na base do tronco (R2=0,46), mas forte (R2=0,72) nos pontos de 1,30 e 3,10 m. O método Pilodyn foi suficientemente confiável que permitiu o desenvolvimento de uma equação para a determinação indireta do DBM do pau-de-balsa considerando o valor da profundidade de penetração a 1,30 m como uma das variáveis.	
Palavras-Chave: 	Alta Floresta-MT; In situ; Melhoramento florestal; Pilodyn.	
Thesagro: 	Densidade da Madeira; Desenvolvimento Florestal; Floresta; Malvaceae; Melhoramento; Ochroma Pyramidale; Silvicultura.	
Thesaurus Nal: 	Genetic improvement; Silviculture.	
Categoria do assunto: 	K Ciência Florestal e Produtos de Origem Vegetal	
URL: 	http://ainfo.cnptia.embrapa.br/digital/bitstream/doc/1143613/1/2022-cpamt-essh-calibration-pilodyn-instrument-indirect-in-situ-determination-basic-wood-density-balsa.pdf	
Registro original: 	Embrapa Agrossilvipastoril (CPAMT)	
Exemplares: 	CPAMT - (1831-1) - UPC - AP - DD -  -  -  - DIS
CPAF-RR - (16287-1) - UPC - AP - DD -  -  -  - DIS